Technical Specification of ADSS Fiber Optical Cable

## 1. General Information

- Product Type: ADSS Single Jacket Fiber Optical Cable

- Certifications: ISO9001

- Standards: ITU-T Rec. G.657A, IEC 60794, ICEA-596, GR-409, YD/T 1997-2009

## 2. Fiber Specifications

### 2.1 Fiber Types

G.652.D/G.655 (single-mode), 50/125μm/62.5/125μm (multimode)

### 2.2 Key Optical Traits

- Attenuation: ≤0.36dB/km (@1310nm, G.652.D); ≤0.22dB/km (@1550nm, G.652.D); ≤3.0dB/km (multimode @850nm)

- Bandwidth: ≥500MHz·km (50/125μm @850nm); ≥200MHz·km (62.5/125μm @850nm)

- PMD: ≤0.20ps/√km (individual fiber); ≤0.10ps/√km (link design)

- Bending Loss: ≤0.75dB (1550nm, 10mm radius/1 turn); ≤1.5dB (1625nm, 10mm radius/1 turn)

### 2.3 Dimensions

Cladding diameter: 125±0.7μm (G.652.D Normal); core/cladding concentricity error ≤0.5μm

## 3. Cable Structure

- Components: GFRP central strength member, PBT loose tube, Aramid yarn reinforcement, HDPE/MDPE sheath

- Fiber Count: 6-288 fibers (OEM: 12-144 cores)

- Dimensions: Diameter 8.0-20.2mm; weight 75-95kg/km (OEM)

- Water Blocking: Water-blocking tape/yarn for moisture resistance

## 4. Mechanical & Environmental Performance

### 4.1 Mechanical Traits

- Tensile strength: 5000N (50m cable); min. bending radius: 10×OD (no tension)

- Fiber load ≥9N; strain ≥1%; stress ≥100kpsi

### 4.2 Environmental Resistance

- Operating temp: -40°C to +70°C; max wind speed 25m/s (0mm ice load)

- Tests (tensile/crush/impact/temp cycling): Loss change ≤0.1dB (@1550nm); no fiber/sheath damage

- Water penetration: No leakage after 24h submersion

## 5. Key Application & Order Info

- Max Span: 50-150m (110kv max applied voltage)

- MOQ: 100km; Delivery time: 5-25 days; Port: NINGBO CHINA

- Payment Term: 30% TT deposit, 70% balance before shipping

- Customization: Fiber count, structure, marking available per request

## 6. Packing & Marking

- Packing: Wooden drum (Φ1100×750mm); 3-4km/spool (2% tolerance)

- Marking: Sheath printed every 1m (cable type, fiber count, length); fiber colors per EIA/TIA 598B