Technical Specification of ADSS Optical Fiber Cable

## 1. General Information

- Type: ADSS (All-Dielectric Self-Supporting) Single Jacket Optical Fiber Cable

- Certifications: ISO9001

- Length per Spool: 3km or 4km (with a tolerance of more than 2%)

- Packing: Wooden Spool (Φ1100*750mm), covered by plastic buffer sheet, sealed by strong wooden battens. At least 1m of the inside end of the cable is reserved for testing.

- MOQ: 100km

- Delivery Time: 5-25 Days

- Port of Loading: NINGBO CHINA

- Term of Payment: 30% TT as deposit, 70% Balance before shipping

## 2. Fiber Specifications

### 2.1 Fiber Types

- G.652.D

- G.655

- 50/125μm Multimode

- 62.5/125μm Multimode

### 2.2 Optical Characteristics

| Parameter | Details |
| --- | --- |
| Attenuation (@850nm) | 50/125μm: ≤3.0 dB/km; 62.5/125μm: ≤3.0 dB/km |
| Attenuation (@1300nm) | 50/125μm: ≤1.0 dB/km; 62.5/125μm: ≤1.0 dB/km |
| Attenuation (@1310nm) | G.652.D: ≤0.36 dB/km; G.655: ≤0.40 dB/km |
| Attenuation (@1550nm) | G.652.D: ≤0.22 dB/km; G.655: ≤0.23 dB/km |
| Bandwidth (@850nm) | 50/125μm: ≥500 MHz·km; 62.5/125μm: ≥200 MHz·km |
| Bandwidth (@1300nm) | 50/125μm: ≥1000 MHz·km; 62.5/125μm: ≥600 MHz·km |
| Polarization Mode Dispersion (PMD) - Individual Fiber | G.652.D: ≤0.20 ps/√km; G.655: ≤0.20 ps/√km |
| PMD - Design Link Value (M=20, Q=0.01%) | G.652.D: ≤0.10 ps/√km; G.655: ≤0.10 ps/√km |
| Mode Field Diameter (@1310nm) | G.652.D Normal: 8.6±0.4μm; G.652.D Best: 9.0±0.4μm; G.657.A1: 9.0±0.3μm; G.657.A2: 8.6±0.4μm |
| Mode Field Diameter (@1550nm) | G.652.D Normal: 9.8±0.5μm; G.652.D Best: 10.2±0.4μm; G.657.A1: 10.2±0.4μm; G.657.A2: 9.6±0.5μm |
| Zero Dispersion Wavelength | 1300-1324 nm for all variants |
| Dispersion Coefficient (1285-1339nm) | G.652.D: ≤3.4 ps/(nm·km); G.657.A1 & A2: ≤3.4 ps/(nm·km) |
| Point Discontinuity (1310nm & 1550nm) | ≤0.05 dB for all fibers |

### 2.3 Transmission Wavelength Bands

- O Band (1260-1360 nm): 237.9-220.4 THz, typically for multimode systems

- E Band (1360-1460 nm): Less commonly used due to higher attenuation

- S Band (1460-1530 nm): 205.3-195.9 THz, used in Passive Optical Networks (PON)

- C Band (1530-1565 nm): 195.9-191.6 THz, widely used for long-haul transmission (minimum attenuation)

- L Band (1565-1625 nm): 191.6-184.5 THz, for extended reach and high-capacity networks

- U Band (1625-1675 nm): 184.5-179.0 THz, primarily for network monitoring

### 2.4 Attenuation Coefficient at Various Wavelengths

- 1310 nm: G.652.D Normal ≤0.35 dB/km; G.652.D Best ≤0.34 dB/km; G.657.A1 & G.657.A2 ≤0.34 dB/km

- 1285-1330 nm: All fibers ≤0.37 dB/km

- 1383 nm: G.652.D Normal & Best ≤0.30 dB/km; G.657.A1 & G.657.A2 ≤0.31 dB/km

- 1490 nm: G.652.D Best ≤0.23 dB/km; G.657.A1 & G.657.A2 ≤0.23 dB/km; G.652.D Normal ≤0.24 dB/km

- 1550 nm: G.652.D Normal ≤0.22 dB/km; G.652.D Best ≤0.21 dB/km; G.657.A1 & G.657.A2 ≤0.20 dB/km

- 1525-1575 nm: G.652.D Normal ≤0.22 dB/km; G.652.D Best ≤0.21 dB/km; G.657.A1 & G.657.A2 ≤0.21 dB/km

- 1625 nm: G.652.D Normal ≤0.25 dB/km; G.652.D Best ≤0.24 dB/km; G.657.A1 & G.657.A2 ≤0.22 dB/km

### 2.5 Bending Loss

- 1550 nm: 10 turns (15mm radius) ≤0.25 dB; 100 turns (25mm radius) ≤0.03 dB; 1 turn (10mm radius) ≤0.75 dB; 1 turn (7.5mm radius) ≤0.2 dB; 100 turns (30mm radius) ≤0.05 dB

- 1625 nm: 10 turns (15mm radius) ≤1.0 dB; 1 turn (10mm radius) ≤1.5 dB; 1 turn (7.5mm radius) ≤0.5 dB

## 3. Cable Structure

### 3.1 Core Components

- Fiber Optic: UV fiber G.652.D; @1310nm ≤0.35dB/km; @1550nm ≤0.2dB/km

- Tube Filling Compound: Water Blocking & Moisture Proof Thyrotrophic gel

- Loose Tube: 1.8-2.0mm PBT; outer diameter options: 1.8, 2.0, 2.5mm (adjustable OEM: 1.5|2.0, 1.8|2.3, 2.1|2.3mm)

- Filler FRP: 1.8mm LDPE/PP

- Center Strength Member: 1.8mm GFRP; diameter options: 2.0, 2.5, 2.8, 3.7mm (adjustable OEM: 1.8|2.3, 1.8|2.3, 2.5, 2.8, 3.7, 2.6mm); PE coated available for specific designs

- Water Blocking Tape: 0.28mm thickness

- Binder: 2 wires Polyester Yarns

- Ripcords: 2 wires

- Dielectric Strength Members: Aramid Yarns KEVLAR K49-3000D

- Inner Jacket: 0.9-1.0mm thickness HDPE/MDPE

- Outer Jacket: 1.6-2.0mm thickness HDPE/MDPE; standard thickness 1.8mm (1.5-2.0mm for OEM)

### 3.2 Key Dimensions & Weight

- Cable Outer Diameter: 10.7±0.5mm (adjustable OEM: 8.0|8.5|9.0|10.5|11.0mm)

- 6 fibers: 9.5mm

- 12 fibers: 9.5mm|10mm

- 24 fibers: 12.2mm

- 48 fibers: 13.9mm

- 72 fibers: 17.1mm

- 96 fibers: 20.2mm

- Cable Weight: 85±5kg/km (typical value; varies by design)

- 12-core: 75kg/km

- 24-core and larger: 95kg/km

### 3.3 Fiber Count & Loose Tube Configuration

- Fiber Count Options: 6, 12, 24, 48, 72, 96, 144, 288 fibers (OEM: 12, 24, 48, 96, 120, 144 cores)

- Tubes per Fiber Count:

- 6 fibers: 1x6, 2x6, 4x6

- 8 fibers: 6x8

- 12 fibers: 4x12, 6x12, 8x12, 12x12 (OEM design for 12-core: 3+2+1)

- 24 fibers: 24x12 (OEM design for 24-core, 48-core, etc.: 1+4+1)

## 4. Mechanical Characteristics

- Fiber Strain: ≥1%

- Fiber Load: ≥9 N

- Stress: ≥100 kpsi

- Dynamic Stress Corrosion Susceptibility Factor: ≥20 (unaged & aged: 30 days @85°C, 85% R.H.)

- Coating Strip Force (Peak Value): 1.3-8.9 N

- Fiber Curl: ≥4 m

- Max. Installation Tension: 2400 N (for all core configurations)

- Min. Bending Radius: Without Tension: 10.0 x Cable Diameter; Under Maximum Tension: 20.0 x Cable Diameter

- MAT (Mechanical Test): Tailored to customer requirements; Max Span options: 50m, 80m, 100m, 120m, 150m (120m span for this model, MAT=3300N)

## 5. Environmental Characteristics

- Temperature Range:

- Operation: -40°C to +70°C

- Installation: -20°C to +60°C

- Transport & Storage: -40°C to +70°C

- Climate Conditions: 25m/s wind speed, 0mm Ice Load; no ice formation considered in design

- Dry Heat Aging (30 days @85°C): Attenuation @1310nm & 1550nm ≤0.05 dB/km

- Accelerated Aging (30 days @85°C, 85% R.H.): Attenuation @1310nm & 1550nm ≤0.05 dB/km

- Temperature Cycling: Attenuation @1310nm & 1550nm ≤0.05 dB/km

- Water Soak (30 days @23°C): Attenuation @1310nm & 1550nm ≤0.05 dB/km

## 6. Test Standards & Requirements

### 6.1 Standards Compliance

ITU-T Rec. G.657A, ISO9001, IEC 60794, ICEA-596, GR-409, YD/T 1997-2009

### 6.2 Mechanical & Environmental Tests

| Test Item | Test Method | Acceptance Requirements |
| --- | --- | --- |
| Tensile Strength (IEC 794-1-E1) | Apply 5000N load over 50m cable length | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Crush Test (IEC 60794-1-E3) | Apply 3000N load over 100mm cable for ≥1 minute | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Impact Test (IEC 60794-1-E4) | 5 impact points, 5 times per point; 4.5Nm energy; 12.5mm hammerhead radius; 2s/cycle | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Repeated Bending (IEC 60794-1-E6) | Bend with 20x outer diameter; 250N load; 3s/cycle; 30 cycles | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Torsion (IEC 60794-1-E7) | 1m length; 150N load; ±90° twist angle; 10 cycles; 1min/cycle | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Water Penetration (IEC 60794-1-F5B) | Submerge 3m cable in 1m water for 24 hours | No water leakage from opposite end |
| Temperature Cycling (IEC 60794-1-F1) | +20°C→-20°C→+20°C→+40°C; 24h/step; 2 cycles | Loss change ≤0.1dB @1550nm; no fiber break, no sheath damage |
| Compound Flow (IEC 60794-1-E14) | 30cm sample; 70±2°C; 24 hours | No compound flow |
| Sheath High Voltage Test | Online test with 9kV voltage (dependent on sheath thickness) | No sheath breakdown |

## 7. Marking & Color Codes

### 7.1 Cable Marking

- Printed every 1 meter: [Cable type] N*cores G.652D [Manufacture year] XXXXm

- Marking color: White

- Occasional unclear length marking permitted if neighboring markings are clear

- Both cable ends sealed with heat shrinkable end caps to prevent water ingress

- Custom marking available per client request

### 7.2 Fiber & Binder Color Code (EIA/TIA 598B)

- Blue

- Orange

- Green

- Brown

- Gray

- White

- Red

- Black

- Yellow

- Violet

- Pink

- Aqua

## 8. Additional Specifications

- Max Applied Voltage: 110kv

- Outer Sheath Color: Black (OEM customizable)

- Customization: Other structures, fiber counts, cable diameters, and weights available per customer requirements. Span recalculated based on installation area's climate conditions.