Technical Specification for ADSS Optical Cable

## 1. Product Overview

All-Dielectric Self-Supporting (ADSS) cable is a type of optical fiber cable that can support itself between structures without relying on conductive metal components. It is designed based on span requirements, voltage levels, and tensile force (MAT) to meet various application scenarios.

## 2. Key Parameters

### 2.1 Basic Information

- Type: Single Jacket ADSS Cable

- Fiber Mode: Single-Mode (SM)

- Max Span: 100m

- Max Applied Voltage: 110kv

- Weather Conditions: 25m/s wind speed + 0mm Ice Load

- Length per Spool: 3km or 4km (with a tolerance of more than 2%)

- Packing: Wooden Spool (Φ1100*750mm)

- Minimum Order Quantity (MOQ): 100km

- Delivery Time: 5-25 Days

- Port of Loading: NINGBO CHINA

- Payment Term: 30% TT as deposit, 70% Balance before shipping

### 2.2 Optical Fiber Specifications

#### 2.2.1 Fiber Types Available

- G.652.D

- G.655

- 50/125μm Multimode

- 62.5/125μm Multimode

#### 2.2.2 Attenuation

| Wavelength | Fiber Type | Attenuation Limit |
| --- | --- | --- |
| 850nm | 50/125μm Multimode | ≤ 3.0 dB/km |
| 850nm | 62.5/125μm Multimode | ≤ 3.0 dB/km |
| 1300nm | 50/125μm Multimode | ≤ 1.0 dB/km |
| 1300nm | 62.5/125μm Multimode | ≤ 1.0 dB/km |
| 1310nm | G.652.D | ≤ 0.36 dB/km |
| 1310nm | G.655 | ≤ 0.40 dB/km |
| 1550nm | G.652.D | ≤ 0.22 dB/km |
| 1550nm | G.655 | ≤ 0.23 dB/km |
| 1285-1330nm | All fibers | ≤ 0.37 dB/km |
| 1383nm | G.652.D (Normal & Best) | ≤ 0.30 dB/km |
| 1383nm | G.657.A1 & G.657.A2 | ≤ 0.31 dB/km |
| 1490nm | G.652.D (Best) | ≤ 0.23 dB/km |
| 1490nm | G.657.A1 & G.657.A2 | ≤ 0.23 dB/km |
| 1490nm | G.652.D (Normal) | ≤ 0.24 dB/km |
| 1525-1575nm | G.652.D (Normal) | ≤ 0.22 dB/km |
| 1525-1575nm | G.652.D (Best) | ≤ 0.21 dB/km |
| 1525-1575nm | G.657.A1 & G.657.A2 | ≤ 0.21 dB/km |
| 1625nm | G.652.D (Normal) | ≤ 0.25 dB/km |
| 1625nm | G.652.D (Best) | ≤ 0.24 dB/km |
| 1625nm | G.657.A1 & G.657.A2 | ≤ 0.22 dB/km |

#### 2.2.3 Bandwidth

| Wavelength | Fiber Type | Bandwidth Limit |
| --- | --- | --- |
| 850nm | 50/125μm Multimode | ≥ 500 MHz·km |
| 850nm | 62.5/125μm Multimode | ≥ 200 MHz·km |
| 1300nm | 50/125μm Multimode | ≥ 1000 MHz·km |
| 1300nm | 62.5/125μm Multimode | ≥ 600 MHz·km |

#### 2.2.4 Polarization Mode Dispersion (PMD)

| Parameter | Fiber Type | Limit |
| --- | --- | --- |
| Individual Fiber | G.652.D | ≤ 0.20 ps/√km |
| Individual Fiber | G.655 | ≤ 0.20 ps/√km |
| Design Link Value (M=20, Q=0.01%) | G.652.D | ≤ 0.10 ps/√km |
| Design Link Value (M=20, Q=0.01%) | G.655 | ≤ 0.10 ps/√km |
| PMD Maximum Individual Fiber | All fiber types | ≤ 0.1 ps/√km |
| PMD Link Design Value | All fiber types | ≤ 0.06 ps/√km |

#### 2.2.5 Mode Field Diameter (MFD)

| Wavelength | Fiber Type | MFD |
| --- | --- | --- |
| 1310nm | G.652.D (Normal) | 8.6 ± 0.4 µm |
| 1310nm | G.652.D (Best) | 9.0 ± 0.4 µm |
| 1310nm | G.657.A1 | 9.0 ± 0.3 µm |
| 1310nm | G.657.A2 | 8.6 ± 0.4 µm |
| 1550nm | G.652.D (Normal) | 9.8 ± 0.5 µm |
| 1550nm | G.652.D (Best) | 10.2 ± 0.4 µm |
| 1550nm | G.657.A1 | 10.2 ± 0.4 µm |
| 1550nm | G.657.A2 | 9.6 ± 0.5 µm |

#### 2.2.6 Zero Dispersion Wavelength & Dispersion Coefficient

- Zero Dispersion Wavelength: 1300-1324 nm for all variants

- Dispersion Coefficient (1285-1339 nm): G.652.D, G.657.A1 & A2 ≤ 3.4 ps/(nm·km)

#### 2.2.7 Point Discontinuity

- At 1310 nm & 1550 nm: ≤ 0.05 dB for all fibers

### 2.3 Physical Dimensions

| Parameter | Specification |
| --- | --- |
| Cladding Diameter - G.652.D (Normal) | 125 ± 0.7 µm |
| Cladding Diameter - G.652.D (Best), G.657.A1, G.657.A2 | 125 ± 0.5 µm |
| Core/Cladding Concentricity Error - G.652.D (Normal) | ≤ 0.5 µm |
| Core/Cladding Concentricity Error - G.652.D (Best), G.657.A1, G.657.A2 | ≤ 0.4 µm |
| Cladding Non-circularity - G.652.D (Normal) | ≤ 1.0% |
| Cladding Non-circularity - G.652.D (Best), G.657.A1, G.657.A2 | ≤ 0.7% |
| Coating Diameter - G.652.D (Normal & Best) | 245 ± 5 µm |
| Coating Diameter - G.657.A1 & G.657.A2 | 242 ± 5 µm |
| Coating/Cladding Concentricity Error - G.652.D (Normal & Best) | ≤ 12 µm |
| Coating/Cladding Concentricity Error - G.657.A1 & G.657.A2 | ≤ 8 µm |
| Loose Tube Outer Diameter | 1.8, 2.0, 2.5 mm (Adjustable: 1.5 |
| Cable Outer Diameter - 6 fibers | 10.7±0.5 mm (Typical); 9.5 mm (Alternative); Adjustable 8.0 |
| Cable Outer Diameter - 12 fibers | 9.5mm |
| Cable Outer Diameter - 24 fibers | 12.2mm |
| Cable Outer Diameter - 48 fibers | 13.9mm |
| Cable Outer Diameter - 72 fibers | 17.1mm |
| Cable Outer Diameter - 96 fibers | 20.2mm |
| Cable Weight | 85±5kg (Typical); 75kg/km (12-core); 95kg/km (24-core and larger configurations) |

### 2.4 Structural Components

- Fiber Optic: UV fiber G.652.D

- Tube Filling Compound: Water Blocking & Moisture Proof Thyrotrophic gel

- Loose Tube: 1.8-2.0 mm PBT

- Filler FRP: 1.8 mm LDPE / PP

- Center Strength Member: 1.8 mm GFRP (Material: Glass Fiber Reinforced Plastic Rod; Diameter options: 2.0, 2.5, 2.8, 3.7 mm; Adjustable: 1.8|2.3, 1.8|2.3, 2.5, 2.8, 3.7, 2.6 mm; PE Coated: Optional)

- Water Blocking Tape: 0.28mm thickness

- Binder: 2 wires Polyester Yarns

- Ripcords: 2 wires

- Dielectric Strength Members: Aramid Yarns KEVLAR K49-3000D

- Inner Jacket: 0.9-1.0mm thickness HDPE / MDPE

- Outer Jacket: 1.6-2.0mm thickness HDPE / MDPE (Thickness standard: 1.8mm; 1.5-2.0mm for customization)

- Peripheral Strength Member: Aramid Yarn

### 2.5 Fiber Count & Loose Tube Configuration

#### 2.5.1 Fiber Count Options

6, 12, 24, 48, 72, 96, 144, 288 fibers; OEM options: 12, 24, 48, 96, 120, 144 cores

#### 2.5.2 Loose Tube Configuration

- 6 fibers: 1x6, 2x6, 4x6

- 8 fibers: 6x8

- 12 fibers: 4x12, 6x12, 8x12, 12x12; OEM design: 3+2+1 (for 12-core)

- 24 fibers: 24x12; OEM design: 1+4+1 (for 24-core, 48-core, and other configurations)

### 2.6 Temperature Range

- Operation: -40°C to +70°C

- Installation: -20°C to +60°C

- Transport & Storage: -40°C to +70°C

- Standard Range (Alternative): -20~+65℃

### 2.7 Mechanical Characteristics

| Parameter | Requirement |
| --- | --- |
| Fiber Strain | ≥ 1% |
| Fiber Load | ≥ 9 N (Newtons) |
| Stress | ≥ 100 kpsi (kilo pounds per square inch) |
| Dynamic Stress Corrosion Susceptibility Factor (Unaged & Aged 30 days @ 85°C, 85% R.H.) | ≥ 20 |
| Coating Strip Force (Peak Value) | 1.3 - 8.9 N |
| Fiber Curl | ≥ 4 m |
| Rated Tensile Strength (RTS) | Calculated based on bearing section strength (mainly spinning fiber) |
| Ultimate Tensile Strength (UTS) | >60% RTS |
| Max Allowable Working Tension (MAT) | 40% RTS; Fiber strain ≤ 0.05% (laminated), ≤ 0.1% (central pipe) without additional attenuation |
| Every Day Strength (EDS) | (16~25) % RTS; No fiber strain or additional attenuation |
| Max Installation Tension | 2400 N (for all core configurations) |
| Min Bending Radius - Without Tension | 10.0 x Cable Diameter |
| Min Bending Radius - Under Maximum Tension | 20.0 x Cable Diameter |

### 2.8 Environmental Characteristics

| Test Condition | Attenuation Limit (1310 nm) | Attenuation Limit (1550 nm) |
| --- | --- | --- |
| Dry Heat Aging (30 days @ 85°C) | ≤0.05 dB/km | ≤0.05 dB/km |
| Accelerated Aging (30 days @ 85°C, 85% Relative Humidity) | ≤0.05 dB/km | ≤0.05 dB/km |
| Temperature Cycling | ≤0.05 dB/km | ≤0.05 dB/km |
| Water Soak (30 days @ 23°C) | ≤0.05 dB/km | ≤0.05 dB/km |

## 3. Standards Compliance

- ITU-T Rec. G.657A

- ISO9001

- IEC 60794

- ICEA-596

- GR-409

- YD/T 1997-2009

- EIA/TIA 598B (for fiber color and binder color code)

## 4. Transmission Wavelength Bands

| Band | Wavelength Range | Frequency Range | Application |
| --- | --- | --- | --- |
| O Band | 1260-1360 nm | 237.9-220.4 THz | Typically used in multimode optical fiber systems |
| E Band | 1360-1460 nm | - | Less commonly used due to higher attenuation |
| S Band | 1460-1530 nm | 205.3-195.9 THz | Frequently used in Passive Optical Networks (PON) |
| C Band | 1530-1565 nm | 195.9-191.6 THz | Most widely used for long-haul fiber-optic transmission (minimum attenuation) |
| L Band | 1565-1625 nm | 191.6-184.5 THz | Second lowest attenuation range, used for extended reach and high-capacity networks |
| U Band | 1625-1675 nm | 184.5-179.0 THz | Primarily used for network monitoring |

## 5. Bending Loss

### 5.1 At 1550 nm

- 10 turns of 15mm radius: ≤0.25 dB

- 100 turns of 25mm radius: ≤0.03 dB

- 1 turn of 10mm radius: ≤0.75 dB

- 1 turn of 7.5mm radius: ≤0.2 dB

- 100 turns of 30mm radius: ≤0.05 dB

### 5.2 At 1625 nm

- 10 turns of 15mm radius: ≤1.0 dB

- 1 turn of 10mm radius: ≤1.5 dB

- 1 turn of 7.5mm radius: ≤0.5 dB

## 6. Test Requirements

### 6.1 Mechanical & Environmental Tests

| Test Item | Test Method | Acceptance Requirements |
| --- | --- | --- |
| Tensile Strength (IEC 794-1-E1) | Apply 5000 N load over 50m cable length | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Crush Test (IEC 60794-1-E3) | Apply 3000 N load over 100 mm of cable for ≥1 minute | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Impact Test (IEC 60794-1-E4) | 5 impact points, 5 times per point; Impact energy: 4.5 Nm; Hammerhead radius: 12.5 mm; Impact rate: 2 seconds per cycle | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Repeated Bending (IEC 60794-1-E6) | Bend with 20x outer diameter (OD); 250 N load; Flexing rate: 3 seconds per cycle; 30 cycles | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Torsion (IEC 60794-1-E7) | 1m length; 150 N load; Twist rate: 1 minute per cycle; Twist angle: ±90°; 10 cycles | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Water Penetration (IEC 60794-1-F5B) | Submerge 3m sample in 1m water for 24 hours | No water leakage from opposite end |
| Temperature Cycling (IEC 60794-1-F1) | Temperature steps: +20°C → -20°C → +20°C → +40°C; 24 hours per step; 2 cycles | Loss change ≤0.1 dB at 1550 nm; No fiber break or sheath damage |
| Compound Flow (IEC 60794-1-E14) | 30cm sample; 70°C ± 2°C; 24 hours | No compound flow |
| Sheath High Voltage Test | Online test with 9 kV voltage (dependent on sheath thickness) | No sheath breakdown |

## 7. Cable Marking & Fiber Colors

### 7.1 Cable Marking

- Marking Content: Fiber cable name, N*cores, G.652D, Manufacture year, Length (XXXXm)

- Marking Interval: Every 1 meter

- Marking Color: White

- Special Note: Occasional unclear length marking is permitted if neighboring markings are clear; Both cable ends are sealed with heat shrinkable end caps to prevent water ingress; Custom marking is available.

### 7.2 Fiber Color and Binder Color Code (per EIA/TIA 598B)

- Blue

- Orange

- Brown

- Gray

- White

- Red

- Black

- Yellow

- Violet

- Aqua

- Pink

- Green

## 8. Features and Applications

### 8.1 Features

- High tensile strength

- All dielectric structure and semi-dry core design

- Small diameter and light weight

- Self-supporting aerial installation

### 8.2 Applications

- Short Span Aerial Installations (e.g., roadside power poles)

- Near High-Voltage Power Lines (safe non-metallic design)

- Telecommunications (long-distance networks, up to 100 km circuits without repeaters)

- Utility Networks (power grid communication)

- Rural Connectivity (broadband in remote areas)

- Military Use (rapid deployment in field communications)

## 9. Customization Options

- Fiber count, structure, cable diameter, and weight can be customized according to customer requirements.

- Span needs to be recalculated based on specific climate conditions of the installation area.

- OEM structure design is available (e.g., core number, strength member material, sheath thickness, etc.).