Technical Specification for ADSS Optical Cable

## 1. General Information

- Type: ADSS-Single Sheath

- Certifications: ISO9001

- Length per Spool: 3km or 4km (2% tolerance allowed)

- Packing: Wooden Spool (Φ1100*750mm)

- MOQ: 100km

- Delivery Time: 5-25 Days

- Port of Loading: NINGBO CHINA

- Payment Term: 30% TT as deposit, 70% Balance before shipping

## 2. Optical Fiber Specifications

### 2.1 Fiber Types

- G.652.D (single-mode)

- G.655 (single-mode)

- 50/125μm Multimode

- 62.5/125μm Multimode

### 2.2 Transmission Characteristics

| Wavelength | Attenuation | Bandwidth |
| --- | --- | --- |
| 850nm | 50/125μm: ≤3.0 dB/km; 62.5/125μm: ≤3.0 dB/km | 50/125μm: ≥500 MHz·km; 62.5/125μm: ≥200 MHz·km |
| 1300nm | 50/125μm: ≤1.0 dB/km; 62.5/125μm: ≤1.0 dB/km | 50/125μm: ≥1000 MHz·km; 62.5/125μm: ≥600 MHz·km |
| 1310nm | G.652.D: ≤0.36 dB/km; G.655: ≤0.40 dB/km | - |
| 1550nm | G.652.D: ≤0.22 dB/km; G.655: ≤0.23 dB/km | - |

### 2.3 Polarization Mode Dispersion (PMD)

- Individual Fiber: G.652.D/G.655 ≤0.20 ps/√km

- Design Link Value (M=20, Q=0.01%): G.652.D/G.655 ≤0.10 ps/√km

### 2.4 Mode Field Diameter (MFD)

- 1310nm: G.652.D Normal (8.6±0.4μm); G.652.D Best (9.0±0.4μm); G.657.A1 (9.0±0.3μm); G.657.A2 (8.6±0.4μm)

- 1550nm: G.652.D Normal (9.8±0.5μm); G.652.D Best (10.2±0.4μm); G.657.A2 (9.6±0.5μm)

### 2.5 Point Discontinuity

- At 1310nm & 1550nm: ≤0.05 dB

## 3. Cable Structure

### 3.1 Core Components

- Fiber Optic: UV fiber G.652.D; @1310nm ≤0.35dB/km; @1550nm ≤0.2dB/km

- Tube Filling Compound: Water Blocking & Moisture Proof Thyrotrophic gel

- Loose Tube: 1.8-2.0mm PBT; Outer diameter options: 1.8/2.0/2.5mm (adjustable: 1.5|2.0, 1.8|2.3, 2.1|2.3mm)

- Filler: 1.8mm LDPE/PP (FRP)

- Central Strength Member: 1.8mm GFRP; Diameter options: 2.0/2.5/2.8/3.7mm (adjustable: 1.8|2.3, 2.5, 2.8, 3.7, 2.6mm); PE coated optional

- Water Blocking Layer: 0.28mm thick water blocking tape + 2 water blocking yarns

- Binder: 2 wires Polyester Yarns

- Ripcords: 2 wires

- Dielectric Strength Members: Aramid Yarns KEVLAR K49-3000D

- Inner Jacket: 0.9-1.0mm thick HDPE/MDPE

- Outer Jacket: 1.6-2.0mm thick HDPE/MDPE; Standard thickness 1.8mm (1.5-2.0mm for OEM)

### 3.2 Cable Dimensions & Weight

- Cable Outer Diameter: 10.7±0.5mm (adjustable: 8.0|8.5|9.0|10.5|11.0mm)

- 6 fibers: 9.5mm

- 12 fibers: 9.5mm|10mm

- 24 fibers: 12.2mm

- 48 fibers: 13.9mm

- 72 fibers: 17.1mm

- 96 fibers: 20.2mm

- Cable Weight: 85±5kg/km

- 12-core: 75kg/km

- 24-core & larger: 95kg/km

### 3.3 Fiber Count & Loose Tube Configuration

| Fiber Count | Tube Configuration |
| --- | --- |
| 6 | 1x6, 2x6, 4x6 |
| 8 | 6x8 |
| 12 | 4x12, 6x12, 8x12, 12x12 |
| 24 | 24x12 |
| 48/72/96/144/288 | Customizable |

## 4. Mechanical Characteristics

- Fiber Strain: ≥1%

- Fiber Load: ≥9N

- Stress: ≥100kpsi

- Dynamic Stress Corrosion Susceptibility Factor: ≥20 (unaged & aged: 30 days @85°C, 85% R.H.)

- Coating Strip Force (Peak Value): 1.3-8.9N

- Fiber Curl: ≥4m

- Max Installation Tension: 2400N (all core configurations)

- Min Bending Radius: Without tension (10x cable diameter); Under max tension (20x cable diameter)

- Max Span: 50m/80m/100m/120m/150m (80m standard for 24F model)

- MAT (Mechanical Test): 2100N

### 4.1 Mechanical Tests

| Test Item | Method | Acceptance Requirement |
| --- | --- | --- |
| Tensile Strength | 5000N load over 50m cable | ≤0.1dB loss @1550nm; No fiber break/sheath damage |
| Crush Test | 3000N load over 100mm for ≥1min | ≤0.1dB loss @1550nm; No fiber break/sheath damage |
| Impact Test | 5 points, 5 times/point; 4.5Nm energy | ≤0.1dB loss @1550nm; No fiber break/sheath damage |
| Repeated Bending | 20x OD bending diameter; 250N load; 30 cycles | ≤0.1dB loss @1550nm; No fiber break/sheath damage |
| Torsion | 1m length; 150N load; ±90° twist; 10 cycles | ≤0.1dB loss @1550nm; No fiber break/sheath damage |

## 5. Environmental Characteristics

- Temperature Range:

- Operation: -40°C to +70°C

- Installation: -20°C to +60°C

- Transport & Storage: -40°C to +70°C

- Weather Conditions: 25m/s wind speed + 0mm Ice Load

- Max Applied Voltage: 110kv

### 5.1 Environmental Tests

| Test Item | Condition | Attenuation Requirement |
| --- | --- | --- |
| Dry Heat Aging | 30 days @85°C | ≤0.05dB/km (@1310/1550nm) |
| Accelerated Aging | 30 days @85°C, 85% R.H. | ≤0.05dB/km (@1310/1550nm) |
| Temperature Cycling | +20→-20→+20→+40°C; 2 cycles | ≤0.05dB/km (@1310/1550nm); No fiber break/sheath damage |
| Water Soak | 30 days @23°C | ≤0.05dB/km (@1310/1550nm) |
| Water Penetration | 3m sample in 1m water for 24h | No water leakage |
| Compound Flow | 30cm sample @70±2°C for 24h | No compound flow |
| Sheath High Voltage Test | Online test with 9kV (dependent on sheath thickness) | No sheath breakdown |

## 6. Standards Compliance

- ITU-T Rec. G.657A, G.652.D

- ISO9001

- IEC 60794

- ICEA-596

- GR-409

- YD/T 1997-2009

- EIA/TIA 598B (fiber/binder color code)

## 7. Marking & Color Code

### 7.1 Cable Marking

- Content: Cable name, N*cores, G.652D, manufacture year, length (meter)

- Interval: Every 1 meter

- Color: White

- End Sealing: Heat shrinkable end caps

### 7.2 Fiber Colors (12 Chromatography)

- Blue

- Orange

- Brown

- Gray

- White

- Red

- Black

- Yellow

- Violet

- Aqua

- Pink

- Green

## 8. OEM Customization

- Fiber count: 12/24/48/96/120/144 cores

- Structure design: 3+2+1 (12-core); 1+4+1 (24/48-core etc.)

- Central strength member: FRP/Steel Wire (1.2/1.0mm diameter)

- Outer sheath thickness: 0.8mm (smaller cores); 1.6/1.9mm (larger cores)

- Cable diameter: 9.0mm (12-core); 13mm (24-core & larger)

- Custom cable marking available

Note: Cable diameter and weight are typical values, subject to design variations. Span needs recalculation for specific regional climate conditions. Other structures and fiber counts available on request.